## Slide 1
Mineral physics
Experimental methods
p-V-T equations-of-state (EoS)
Partly based on a presentation by
Peter Lazor, Univ. Uppsala

## Slide 2
Seismic parameter / bulk sound speed:
KS/r = vp2 – 4/3vs2 = F
Shear modulus: G or m
G/r = vs2
vs = (G/r)1/2
vp = (Ks/r + 4/3*G/r)1/2
= [(Ks + 4/3*G) / r]1/2

## Slide 3
Objective:
Relate vP-vS-data to mineralogical and chemical composition of Earth’s interior
We need:
Equations of state (EoS): V = f(p,T) or p = f(V,T)
Example: an ideal gas: pV = nRT
Solids are MUCH more complicated
Helmholtz free energy: F(V,T) = F0(V) + Fvib(V,T) + Fel(V,T)
0 K compression
component
vibrational
component
electronic thermal
exitation component
p(V,T) = p0(V) + pvib(V,T) + pel(V,T)
Pressure: p = –(dF/dV)T
p(V,T) = p0(V) + pthermal(V,T)

## Slide 4
Isothermal bulk modulus: KT = –(Vdp/dV)T = 1/b
Compressibility
p-derivative of KT: KT’ = (dKT/dp)T
Adiabatic / isentropic bulk modulus: KS = –(Vdp/dV)S
KS = KT(1 + Tag)
Thermal
expansivity
~ 2*10-5 K–1
Grüneisen
parameter
g = aKs/(rCp)
~ 1 for silicates
Units:
bulk modulus: GPa
compressibility: GPa-1

## Slide 5
Adiabatic compression law: g = (dT/dr)S = aKS / rCP
g = V/CV (dp/dT)V
Liquid EoS, Mie-Gruneisen form:
p(V,T) = pc(V,T0) + g CV (T-T0)/V
p(V,T) = pc(V,T0) + (dp/dT)V(T-T0)

## Slide 6
The simplest isothermal EoS
Isothermal bulk modulus:
Compressibility:
Integration of: dV/V = - dP/KT →
- does not account for the fact that it is increasingly difficult to
compress a solid at increasing p, i.e. KT increases with p
- here KT is constant and equal to K0 (the zero pressure value)
where V0 is zero pressure volume
Notes: 6

## Slide 7
Murnaghan linear EoS
Assumption: K varies linearly with pressure K = K0 + K’*p
p-derivative of K: K’ = dK/dp
Generally limited to b < 10%, i.e. V/V0 > 0.9.
Reproduces p-V data and the value of K0
- Simple EoS, allowing algebraic solutions of V = f(p) and p= f(V)
- Commonly incorporated in thermodynamic databases
Notes: 7

## Slide 8
Finite strain EoSs
- strain energy of a compressed solid expressed as a Taylor series of finite strain, f
- several alternative definitions of f → different p-V-relationships
Birch-Murnaghan Equation of State
The Birch-Murnaghan EoS
- based on Eulerian strain, fE = [(V/V0)2/3 – 1]/2
- expansion to 4th order in the strain yields the following EoS:
Notes: 8

## Slide 9
Third- and second-order Birch-Murnaghan EoS
Truncation to 3rd order:
Implied value of K’’:
Common isothermal EoS-expressions used in high-pressure studies
K’ = 4: Second-order Birch-Murnaghan EoS
= 0
Fourth-order B-M:
Third-order B-M:
Eulerian strain,
fE = [(V/V0)2/3 – 1]/2
Notes: 9

## Slide 10
The fit of p-V data to the 3rd order Birch-Murnaghan EOS
solid squares – this work
dots with error bars – Haavik et al. (2000)
The dotted lines represent the 90% confidence limits for the fit.
’
MAGNETITE
Notes: 10

## Slide 11
Notes: 11

## Slide 12
(Anderson and Ahrens, 1994)
Presence of light
element(s) in the
outer core required.
Pure Fe is too dense.
Liquid Fe
Notes: 12

## Slide 13
Thermal Equations of State
Simple method for evaluating p-V-T data
isothermal EoS (e.g. M, BM or Vinet), with V0 and K0 as material properties
at p = 0 and high T
derived by integration of the
expression for the thermal expansivity:
Common approximations
a(T) = C (constant) or
a(T) = a + bT
Higher-order terms can be used when necessary
Isothermal, third-order BM EoS
High-T V0 (zero-pressure V):
Notes: 13

## Slide 14
Neutral buoyancy between:
MgSiO3-rich bridgmanitic material (0-4 mol% FeSiO3 + FeAlO3) and PREM (or pyrolite)
At 120 GPa and DT=0:
Dr = 2.5 for 2 mol% FeSiO3 and Dr = 1.5 for 5 mol% FeSiO3
BM, third-order:
Dp = 1.5 K0 [(Dr0 / Dr)2.33 - (Dr0 / Dr)1.67] [1 - 0.75(4-K'){(Dr0 / Dr)0.67 -1}]
BM, second-order
Dp = 1.5 K0 [(Dr0 / Dr)2.33 - (Dr0 / Dr)1.67] [(Dr0 / Dr)0.67 -1]
What is Dp for: Dr0 = 0.5
2 mol% FeSiO3: Dp = 1.5 257 [(0.2)2.33 - (0.2)1.67] [(0.2)0.67 -1] =
5 mol% FeSiO3: Dp = 1.5 257 [(0.333)2.33 - (0.333)1.67] [(0.333)0.67 -1]
r = m/V, V = m/r
V/V0 = m/r / m/r0 = r0 / r
Isothermal, third-order BM EoS

## Slide 15
Within uncertainties of current experimental measurements, the variation of K0(T) is approximately linear:
This formulation, combined with use of a variable K’ in the associated isothermal EoS, includes all second derivatives of the volume with respect to the intensive variables P and T, and is usually sufficient to fit most experimental P-V-T datasets collected from room temperature up to ~1000 K.
Ref. temp. T0:
mostly 289 K
Notes: 15

## Slide 16
Data sets:
this work
Okudera (1996)
Fei et al. (1999)
Olsen (1994)
Shebanova and Lazor (2003)
dKT/dT = -0.030(5) GPa/K
p-V-T equation of state of magnetite
(high temperature BM-EOS after Saxena)
Notes: 16

## Slide 17
G/r = vs2
K/r = vp2 – 4/3vs2 = vf2 = F
vf: bulk sound velocity,
F : seismic parameter
Seismic velocities  physical properties
Bulk modulus: K (= incompressibility / stiffness)
Shear modulus: G
vs2 = G/r
vp2 = (K + 4/3*G)/r

## Slide 18
Bragg's law
positive interference
when nl = 2d sinq
Unit cell V and r
as a function of p
Angle-dispersive XRD
Monochromatic beam, fixed l, variable q
Energy-dispersive XRD
Polychromatic (”white”) beam, fixed q
d-spacings from dispersed energy peaks
E = hf = hc/l
l = hc/E 2d sinq = nl = nhc/E
In-situ high-pT XRD, using
high-intensity synchrotron radiation

## Slide 19
piston
cylinder
gasket
Water-cooled
DAC-holder
c.

## Slide 20
1 cm
Steel gasket
Diamond anvil cell (DAC)

## Slide 21
1 cm
Steel gasket
Diamond anvil cell (DAC)

## Slide 22
Culet diameter: 0.3 mm
From above
From the side
Indented gasket with 100 mm hole og Fe3+-bearing sample
Under pressure, from above

## Slide 23
100 m
Laser heating facility at Univ. of Bristol

## Slide 24
X-ray beam
to detector

## Slide 25
Monochromatizing a ”white” X-ray beam

## Slide 27
Andrault et al. 2011, Nature

## Slide 28
Example of LH-DAC-experimentation with in-situ, synchrotron-based XRD:
Phase relations of aluminous silica to 120 GPa
Extreme Conditions Beamline
(P02.2), PETRA-III,
DESY, Hamburg
Andrault et al.
(2014, Am. Mineral.)

## Slide 29
Andrault et al.
(2014, Am. Mineral.)

## Slide 30
High-pressure experimental methods: Piston cylinder and multianvil technology

## Slide 32
Piston
WC-core (of pressure plate)
containing the central
cylindrical pressure chamber
Supporting steel rings
Supporting steel rings
Base plug support plate
Siff mylar electric insulation

## Slide 36
Multi-anvil, sintered diamond technology, ETH, Zurich:
True split-cylinder, 6-8-configuration (design of Kawai & Endo, 1970)
1 mm
1 mm
1 mm
Corner truncation on
sintered diamond cube

## Slide 40
ISEI, Okayama Univ., Misasa
ETH, Zurich
ETH, Zurich

## Slide 41
BGI, Bayreuth
SUNY, Stony Brook

## Slide 43
Walker (1989)-type 6-8-configuration design,
Inst. of Meteoritic, Univ New Mexico (C. Agee, D. Draper)

## Slide 48
Spring-8, JSRI, Japan

## Slide 49
Deformation-DIA-apparatus
Cubic-anvil apparatus